| P.O. BOX 1120 |  |  | PH: 800 324-1806 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| BRAMPTON, ONTARIO, CANADA L6V 2L8 |  |  | PH: 905 453-4100 |  |  |  |
| # ZOCO 103 |  |  |  |  | ## ZOCHEM ZINC OXIDE |  |
| FRENCH PROCESS ZINC OXIDE |  |  |  |  |  |  |
| PRODUCED FROM PRIMARY GRADE ZINC |  |  |  |  |  |  |
| DESCRIPTION |  |  |  |  |  |  |
| ZOCO 103 is a large particle size, high purity, zinc oxide excellent for applications where low surface area and low reactivity is required |  |  |  |  |  |  |
| USES |  |  |  |  |  |  |
| Rubber, Paint, Ceramics, Chemicals, Adhesives, Lubricants |  |  |  |  |  |  |
| ## TYPICAL TECHNICAL VALUES** |  |  |  |  |  |  |
| CHEMICAL PROPERTIES (%) |  |  |  | MAXIMUM | MINIMUM最低值 | TYPICAL |
| Zinc Oxide (ignited basis) 氧化锌 |  |  |  | n/a | 99.9 | 99.9 |
| Lead (Pb) 铅 |  |  |  | 0.0024 | n/a | 0.0015 |
| Cadmium (Cd)镉 |  |  |  | 0.0010 | n/a | 0.0003 |
| Copper (Cu)铜 |  |  |  | 0.0005 | n/a | 0.0001 |
| Iron (Fe)铁 |  |  |  | 0.0005 | n/a | 0.0002 |
| Loss at 110 degrees C 烧失量 |  |  |  | 0.15 | n/a | 0.05 |
| PHYSICAL PROPERTIES |  |  |  | MAXIMUM | MINIMUM | TYPICAL |
| Surface Area (m 2/g)比表面积 |  |  |  | 3.99 | n/a | 3.50 |
| Particle Size (microns)粒径 |  |  |  | n/a | 0.27 | 0.31 |
| Bulk/Tapped Density (lb/cu. ft)松密度 |  |  |  |  |  | 50 |
| Oil Absorption (ml oil/100g ZnO)吸油值 |  |  |  |  |  | 16.0 |
| Screen Test - Through 325 Mesh (%)过325目筛 |  |  |  | n/a | 99.99 | 99.995 |
| Specifications |  |  |  |  |  | ASTM D-79 |
| ** The above specifications are typical for the noted grade. Zochem will produce material to meet specific customer specifications. |  |  |  |  |  | ### REVISION 07: February 24, 2013 |